## Slide 1
Biodegradable packaging as a potent source of biogas following thermal hydrolysis pre-treatment
Dr Andrew Walsh

## Slide 2
The Reality of Bio-waste

## Slide 3
Aerobic Composting of Biodegradable Packaging

## Slide 4
?
“Wet” AD of biodegradable packaging
In Europe “AD” current represents
between 30-70% of the bio-waste
recycling infrastructure.
The balance of the capacity is
composting.
This balance is shifting towards
AD due to the incentivized
production of a sustainable
biofuel in the form of biomethane.

## Slide 5
“Wet” AD of Biodegradable Packaging

## Slide 6
Thermo-pressure hydrolysis (TPH)
120 -185 oC
2 – 6 bar steam pressure
20 – 40-minute treatment
&
Hemicellulose
Soluble sugars

## Slide 7
7
TPH
TPH of packaged bio-waste and removal of plastics
Screen

## Slide 8
Thermo-pressure hydrolysis (TPH)

## Slide 9
Biomethane from Food waste (with and without TPH)

## Slide 10
392 m3/t VS
180 m3/t waste
79% Extraction
Trial 1 - Biodegradable AD Reject

## Slide 11
Trial 2 - Biodegradable AD Reject
350 m3/t VS
100 m3/t waste
45% Extraction

## Slide 12
Trial 3 - Mixed biodegradables
387 m3/t VS
317 m3/t waste
100% Extraction

## Slide 13
Trial 4 - Impact of TPH on Hydrocarbon Plastics

## Slide 14
Trial 5 – Bio-packaging components

## Slide 15
85.6% pass
PLA Coffee pods with coffee
Lids did no pass
96.7% pass
Cellulosic carrier bags
(Corn starch)
90.4% pass
General packaging composed of “biomass” - bagasse, wood and cardboard
Bio-packaging liquefied by thermal hydrolysis
100% Pass
PLA material

## Slide 16
Bio-packaging not liquefied by thermal hydrolysis
Bioplastics other than PLA that are designed for high temperature applications (cooking) did not liquefy or fragment significantly.
Therefore, this class of bioplastics can be expected to rejected at conventional and TPH AD facilities prior to digestion.
However, this grade of bio-plastic appears to represent a relatively small proportion of biodegradable packaging on the market.

## Slide 17
Biomethane potential of the various bio-materials
Chart: Methane per tonne (fresh weight)
| Coffee pods | Bio-bags | Pods & bags | Biomass mix | Biomass mix (c) | Food waste
fresh weight | 337 | 100 | 271 | 82 | 314 | 110

## Slide 18
The Full-scale experience

## Slide 19
Derby “Food waste”

## Slide 20
Performance
Chart: 
| Food waste | Food waste (TPH) | Cardboard | Cardboard (TPH)
 | 70 | 90 | 20 | 180
Methane
m3/t

## Slide 21
TPH versus conventional digestion modelling
111 m3 CH4/ fresh tonne
155 m3 CH4/ fresh tonne
4,000 tpa of waste to landfill
1,400 tpa of waste to landfill

## Slide 22
1 tonne of mixed biodegradable packaging = 310 m3 CH4
(TPH) = 3.1 MWth
Renewable energy potential of bio-packaging
3.1 MWth = 100 household daily consumption
3.1 MWth = 310 litres of diesel
= 5,000 km for an average car
1 tonne of typical food waste (no TPH) = 130 m3 CH4
= 1.3 MWth

## Slide 23
Questions?